## Slide 1: Polymeric-based Therapeutics for Gene Delivery Against Cancer
    Corey J. Bishop, Ph.D.
    Principal Investigator of the Pharmacoengineering Laboratory
    www.pharmacoengineering.com
    April 20, 2018

## Slide 2: Nanomedicine
http://www.particlesciences.com/images/tb/size-comparison.jpg

## Slide 3: Nanomedicine
http://www.particlesciences.com/images/tb/size-comparison.jpg

## Slide 4: Nanomedicine
http://www.particlesciences.com/images/tb/size-comparison.jpg

## Slide 5: Gene Therapy is Challenging
Regulatory Approvals for Gene Therapy
  CFDA (2003)
  EMA (2012)
  U.S. FDA (2017)
Viruses vs. non-viral
gene delivery vectors
  Effective vs. safe
Sunshine, Bishop, Green, Ther. Delivery 2011
Notes: “The area of nanomedicine I am most interested in is”…
HNSCC: head and neck squamous cell carcinoma
LPL: lipoprotein lipase for hypertriglyceridemia
EMA: european medicines agency
Regulatory Bodies
  CFDA in China in 2003
    Adenovirus-P53 for HNSCC
  EMA in EU in 2012
    Assoc-Adenovirus LPL into muscle cells
Need safer
more effective
vectors
Discuss mechanism

## Slide 6: Advantages and Disadvantages of Non-viral and Viral Gene Delivery Vectors
Pros
  Less insertional mutagenesis
  Less immunogenicity
  Easy to scale synthesis up
  Easy to chemically modify
  Relatively cheaper
Cons
  Less effective
  Temporary expression (Pro?)
Non-viral vectors
Viral vectors
Pros
  More effective
  Permanent expression
Cons
  More insertional mutagenesis
  More immunogenicity
  Difficult to scale synthesis up
  Relatively expensive

## Slide 7: Gene Therapy: Promising
Root cause of many inheritable diseases and cancer is genetic Treatment

## Slide 8: Gene Therapy: Promising
Root cause of many inheritable diseases and cancer is genetic Treatment
Central Dogma:
DNA mRNA Protein
Function:
Pro-apoptotic or Pro-inflammatory
(i.e., TRAIL, HSV-TK, IL-2,4,12, IFNβ, GM-CSF)

## Slide 9: Gene Therapy: Promising
Root cause of many inheritable diseases and cancer is genetic Treatment
Central Dogma:
DNA mRNA Protein
siRNA mRNA Protein
RISC
Function:
Pro-apoptotic or Pro-inflammatory
(i.e., TRAIL, HSV-TK, IL-2,4,12, IFNβ, GM-CSF)
Anti-function:
Anti-growth factor or anti-migratory
(anti-EGF, anti-Robo)

## Slide 10
Notes: Re-show what I did initially and then move on.

## Slide 11
Sub-Aim A
Notes: Re-show what I did initially and then move on.

## Slide 12
Binding
Sub-Aim A
Notes: Re-show what I did initially and then move on.

## Slide 13
Binding
Diameter
Sub-Aim A
Notes: Re-show what I did initially and then move on.

## Slide 14
Binding
Zeta potential
Diameter
Sub-Aim A
Notes: Re-show what I did initially and then move on.

## Slide 15
Binding
Zeta potential
Expression
Viability
Diameter
Sub-Aim A
Notes: Re-show what I did initially and then move on.

## Slide 16
  Mn, Mw, PDI, DP, B:S, B, S, B+S, BP, MP, CV, GFE, LogP, MR, HtF, tPSA
Expression
Viability
Uptake
Sub-Aim C
Notes: Re-show what I did initially and then move on.

## Slide 17: Sub-Aim A
Aim: Quantifying how poly(beta-amino ester) (PBAE) structural properties affect polymer/DNA binding thermodynamics and gene delivery
Control Function
  High throughput vs Design
Structure-Function Relationship
  Further mechanistic understanding
  Improve polymeric materials
Notes: polymer/DNA binding thermodynamics and

## Slide 18: Structure-Function Assessment
Notes: Point out the amine for charge for complexation and buffering and ester for hydrolytic degradation
Explicitly state that b and sX are the number of carbons in the monomer.

## Slide 19: Time-correlated single photon counting: ethidium bromide
Lamp (background)
Time (ns)
# of Counts
Notes: Point out this is a histogram
What you are looking at here is the emission responses of ethidium bromide at different wavelengths. We are able to fit 2 exponential terms summed to the responses observed which are associated with the 2 different fluorescing entities namely ethidium bromide bound and unbound to DNA. If all of the ETB were bound or unbound to DNA we would only have 1 term.

## Slide 20: Time-correlated single photon counting: ethidium bromide
Time (ns)
Lamp (background)
# of Counts
Curve Fitting: Global decay constants;
Amplitude varies with wavelength (560-670 nm)
Notes: Point out this is a histogram
What you are looking at here is the emission responses of ethidium bromide at different wavelengths. We are able to fit 2 exponential terms summed to the responses observed which are associated with the 2 different fluorescing entities namely ethidium bromide bound and unbound to DNA. If all of the ETB were bound or unbound to DNA we would only have 1 term.

## Slide 21
Chart: wavelength (nm)
| 670 | 650 | 640 | 630 | 620 | 610 | 600 | 590 | 580 | 560
1.81 ns | 0.02241 | 0.022519 | 0.023877 | 0.023787 | 0.023362 | 0.020454 | 0.018068 | 0.015489 | 0.012636 | 0.0061848
22.58 ns | 0.032575 | 0.041124 | 0.048469 | 0.055484 | 0.062355 | 0.068117 | 0.063217 | 0.055709 | 0.042468 | 0.013823
Unbound ETB
DNA Bound ETB
Decay-Associated Spectra

## Slide 22
Chart: wavelength (nm)
| 670 | 650 | 640 | 630 | 620 | 610 | 600 | 590 | 580 | 560
1.81 ns | 0.02241 | 0.022519 | 0.023877 | 0.023787 | 0.023362 | 0.020454 | 0.018068 | 0.015489 | 0.012636 | 0.0061848
22.58 ns | 0.032575 | 0.041124 | 0.048469 | 0.055484 | 0.062355 | 0.068117 | 0.063217 | 0.055709 | 0.042468 | 0.013823
Unbound ETB
DNA Bound ETB
A1
A2
Decay-Associated Spectra

## Slide 23
Chart: wavelength (nm)
| 670 | 650 | 640 | 630 | 620 | 610 | 600 | 590 | 580 | 560
1.81 ns | 0.02241 | 0.022519 | 0.023877 | 0.023787 | 0.023362 | 0.020454 | 0.018068 | 0.015489 | 0.012636 | 0.0061848
22.58 ns | 0.032575 | 0.041124 | 0.048469 | 0.055484 | 0.062355 | 0.068117 | 0.063217 | 0.055709 | 0.042468 | 0.013823
Unbound ETB
DNA Bound ETB
A1
A2
Decay-Associated Spectra

## Slide 24
Decay-Associated Spectra
Chart: wavelength (nm)
| 670 | 650 | 640 | 630 | 620 | 610 | 600 | 590 | 580 | 560
1.81 ns | 0.02241 | 0.022519 | 0.023877 | 0.023787 | 0.023362 | 0.020454 | 0.018068 | 0.015489 | 0.012636 | 0.0061848
22.58 ns | 0.032575 | 0.041124 | 0.048469 | 0.055484 | 0.062355 | 0.068117 | 0.063217 | 0.055709 | 0.042468 | 0.013823
Unbound ETB
DNA Bound ETB
A1
A2
Hill Equation:

## Slide 25: Binding constants
(A), backbone (B), sidechain (C), and endcaps (D).
One-way ANOVA / Tukey post-hoc2
Notes: “average bc” - mao

## Slide 26
Glioblastoma Cells
MDA-MB-231 Cells

## Slide 27: Conclusions
Binding constants 1-6E4 M-1 for PBAEs are optimal in both human cancer cell lines tested and biphasic with respect to transfection efficacy
Binding constant in this range is necessary but not sufficient for effective transfection
Binding affinity is tunable
No strong trends between diameter/ZP and transfection
Bishop, et al. J. Am. Chem. Soc. 2013, 135, 6951-6957.
Ketola, Hanzlikova, Leppanen, Ravina, Bishop, et al. J. Phys.Chem. B. 2013, 117, 10405-13.

## Slide 28: Principal Component Analysis: Sub-Aim C
Reduces complex data => linearly uncorrelated orthogonal components
Typically: Av = λv

## Slide 29: Principal Component Analysis
Reduces complex data => linearly uncorrelated orthogonal components
Typically: Av = λv
(A – 11TA(1/n) = C)TC = M
M = variance-covariance matrix
Mv = λv; v = eigenvectors; λ = eigenvalues
Mv = scores: inter-variable correlations
v = coefficients rank variables’ contributions

## Slide 30: Normalized Variables
Physico-chemical properties:
  Mn, Mw (MW*), PDI, DP, B:S, B, S, B+S
  Joback/Crippen’s Fragmentation method: BP*, MP*, CV*, GFE*, LogP*, MR*, HtF*, tPSA
  * = repeating unit (vs full polymer)
Cellular function
  Viability, uptake, transfection

## Slide 31
Figure 1. Top: the variances are explained for the first5 PCs. The top 4 variables of the 27 are ranked by the degree to which they contribute to the PCs
according to their associated coefficients and listed above the variances. The “(-)” indicates a negative contribution; Bottom: The loading plot of all of the
variables showing relative correlations.
Figure S1
Notes: Mention some variables line up with PC1 and other variables line up with PC2 and some are in between.

## Slide 32: Variables driving function
Ranking of variables: Acos(Θ) = correlation strength
E number index was most neutral in all cases: 0.02, 0.01, -0.01.

## Slide 33: Scores Plot
B+S
Mn
Mw
Notes: “Self-assembled”

## Slide 34: Red = highest transfection level
The scores plot versus transfection efficacy with red being the highest level of transfection; B: region B of 3A with a B+S (sum of carbons in backbone and sidechain) value of 7;
C: region C of 3A with a B+S value of 8; D: region D of 3A with a B+S value of 9.
Notes: “Self-assembled”

## Slide 35: Conclusions
(+)-correlations:
  Transfection
    B, uptake, LogP*, B+S
  Uptake
    LogP*, B+S, GFE*, MW*
  Viability
    HtF*, B:S, HtF, GFE
(-)-correlations:
  Transfection
    GFE, HtF, HtF*, B:S
  Uptake
    GFE, HtF, B:S, HtF*
  Viability
    MP*, CV*, MR*, LogP*
LogP*, B+S drive uptake/transfection
PCA is a useful tool for helping elucidate which and to what degree structural properties drive cell-based function
Bishop, et al. Chemical Communications. 2015. 51, 12134-12137.

## Slide 36: Acknowledgements: Thank You!
Green Lab
  Dr. Jordan Green
  Dr. Stephany Tzeng
  Dr. Joel Sunshine
  Dr. Nupura Bhise
  Dr. Ron Shmueli
  Kristen Kozielski
  Jay Kim
  Randall Meyer
  David Wilson
  Toni Guiriba
  Rebecca Majewski
  Richard “Josh” Murdock
  Allen Liu
  David Lee
  Evan Smith
Thesis Committee
Dr. Jordan J. Green
Dr. Hai-Quan Mao
Dr. Warren Grayson
Dr. Kevin Yarema
Collaborators
Dr. Tiia Ketola
Dr. Elina Vuorimaa
Dr. Marjo Yliperttula
Dr. Ting Wang
Dr. Gregg Semenza
Funding:
NSF GRF to CB: DGE-0707427
NIH: 1R01EB016721,
R21CA152473
Tekes PrinCell II 40050/09 FI
Wilmer Core Grant: EY001765,
P30-EY001865
Gates’ Foundation
Langer Lab
  Dr. Bob S. Langer
  Dr. Adam M. Behrens
  Dr. Kevin J. McHugh
  Dr. Ana Jaklenec
  Xiao Le
  Dr. Thanh Nguyen
  Dr. Stephany Tzeng
  Dr. Shiran Ferber

## Slide 37: Overview
Specific Aim: Elucidate structure-function relationships of a polymeric non-viral gene delivery system used for glioblastoma and triple-negative breast cancer applications:
  Sub-Aim 1: Polyplex binding correlations in cancer (Bishop, et al. JACS)
  Sub-Aim 2: Structure-function elucidation via PCA (Bishop, et al. Chemical Commun.)
  Sub-Aim 3: Cellular and nuclear uptake rates and differential equation modeling in cancer (Bishop, et al. Acta Biomaterialia)

## Slide 38
kcell
Sub-Aim B
Notes: Re-show what I did initially and then move on.

## Slide 39
kcell
kne
Sub-Aim B
Notes: Re-show what I did initially and then move on.

## Slide 40
kcell
kne
kni
Sub-Aim B
Notes: Re-show what I did initially and then move on.

## Slide 41
kcell
kne
kni
kbd
Sub-Aim B
Notes: Re-show what I did initially and then move on.

## Slide 42
kcell
kne
kni
kbd
Structure
Sub-Aim B
Notes: Re-show what I did initially and then move on.

## Slide 43
kcell
kne
kni
kbd
  Mn, Mw, PDI, DP, B:S, B, S, B+S, BP, MP, CV, GFE, LogP, MR, HtF, tPSA
Sub-Aim C
Notes: Re-show what I did initially and then move on.